United States Steel Corporation

Great Lakes Works

Hydrogen Sulfide Abatement plan – A1, B2, & D4 Slag Pits

In order to maintain compliance with Michigan Rule 336.1406(2) which states, “When the odor of Hydrogen Sulfide is found to exist beyond the property line of a source, a person in Wayne County shall not cause or allow the concentration of hydrogen sulfide to exceed 0.005 parts per million by volume for a maximum of 2 minutes”, United States Steel Corporation – Great Lakes Works is proposing to take the following actions:

United States Steel Corporation – Great Lakes Works shall reduce Hydrogen Sulfide Emissions generated at operating blast furnace slag pits which may service cast houses A, B, and/or D by operating and maintaining a hydrogen peroxide (or equivalently effective chemical  as approved by the AQD) feed system which shall feed into the slag pit quench water spray system.

Operating blast furnace slag pits serving cast houses A, B, and/or D shall follow procedures established in SJP 1510-05-19 -  Slag Pit Practices, section 6.2.1.  In the event of a system malfunction, follow procedures established in SJP 1510-05-19 -  Slag Pit Practices, section 6.2.1.  System error shall be identified and if possible, immediately corrected.  If system error/problem cannot be immediately corrected, it shall be corrected as quickly as practical.

Daily records shall be kept for a period of not less than 2 years for each of the following:

- Water Flow system operational status

- Hydrogen peroxide or equivalent additive system operating status

Weekly records shall be kept for a period of not less than 2 years for the following:

- Physical hydrogen peroxide or equivalent chemical feed system inspections